## Slide 1: “A STUDY ON STRENGTH AND DURABILITY OF M30 CONCRETE USING GROUNDNUTSHELL ASH AND SISAL FIBER”
Supervisor : Submitted By :
Dr. Vishnu Sharma ABHIJEET SINGH
Professor(CE) En. No.: 18E2YTSTM30P600
Department of Civil Engineering
Yagyavalkya Institute of Technology & Engineering
Sitapura,Jaipur

## Slide 2: Contents
Introduction
Literature Survey
Objectives
Result Analysis
Conclusions
Future Scope
References

## Slide 3: INTRODUCTION
Concrete is a popularly used material in the world. More than 10 billion tons of concrete are consumed annually. Conventional concrete is a blend of cement, sand, aggregate and water.
Groundnut Shell Ash is waste material produced by local markets on shops, carts etc and in large amount by oil industry and many other large scale industry where the shell emerges as waste product. A large of waste is produced by such regular use of groundnut.
This can be used as a construction material by partially replacing cement that can reduce overall cost and in addition to this waste management is also taking place. A little research is done in this field to find the strength properties of Ground Shell Ash utilized concrete.

## Slide 4
Sisal fiber is derived from an agave, Agave sisalana. It is valued for cordage because of its strength, durability, ability to stretch, affinity for certain dyestuffs, and, like coir, it is resistant to deterioration in saltwater. The higher-grade fiber is converted into yarns for the carpet industry. The function of randomly dispersed fibers is to bridge across the cracks that provides some post cracking ductility.

## Slide 5: Literature Survey
1 MALUGU RAVI PRASANTH (2019) The Compressive Strength
and spilt tensile of Concrete is increased when the replacement
of Cement with groundnut shell ash up to 10% replaces by weight of Cement. The Flexural Strength of Concrete is increased when the replacement of Cement with groundnut shell ash up to 15% replaces by weight of Cement

## Slide 6
2. Nadiminti Venkata Lakshmi, Polinati Satya Sagar (2017) this experimental investigation was carried out to evaluate the strength of concrete, in which cement was replaced with ground nut shell ash for cubes, cylinders, and Prisms with different percentages which vary from 0% to 30% at an interval of 5% were performed. These Cubes, cylinders, and prisms were tested for 7, 14 and 28 days for compression, flexural and split tensile strengths. It is observed that 10% replacement of ground nut shell ash shown the highest strength values when compared with other percentages and for 15% replacement of ground nut shell ash the compressive and split tensile strength obtained the highest strength rather than other flexural strength.
3. Jamilu Usman 1 , Nasiru Yahaya , (2013) . This paper presents the effect of groundnut shell ash (GHA) on the properties of cement paste. Cement pastes containing GHA as cement replacement in different proportions up to 50% by weight were prepared. The results show that GHA increased water demand and delayed setting times, but improved soundness of cement paste. Moreover, compressive strength enhancement of hardened cement paste due pozzolanic reaction as evidenced by the microstructure analysis (FTIR) was observed with up to 10% GHA replacing cement.

## Slide 7
4 .DR. F. A. Olutoge1 Buari T.A2 (2013) The principal characteristic measured was the compressive strength of Ordinary Portland Cement (OPC) concrete and OPC/GSA concrete at varying substitution levels of 0%, 5%, 10% and 15% after curing in water and three chemical solutions (MgSO4 , NaSO4 and Ca2 SO4 ) of varying concentrations of 0.5%, 1.5% and 2.5% each at 56 day hydration period. The results showed that the OPC/GSA concrete performed best in these chemical solutions, especially at 10% GSA replacement which exhibited a convincing increase in compressive strengths above that obtain with the use of Ordinary Portland cement
.
5. T.C. Nwofor and S. Sule (2012) this study investigates the use of considerable volume of groundnut shell ash as the partial replacement for cement in concrete production. A total of 100 specimens of the GSA/OPC concrete was cured in cubes of 100mm dimension for 7, 14, 21 and 28 days and the compressive strength and density determined. The percentage replacement of Ordinary Portland Cement (OPC) varies to the control (0% replacement) about 40%. The results generally show a decrease in density and compressive strength as the percentage replacement with GSA increases suggesting less hydration with cement. Based on a general analysis of the results as well as the logical comparison to the acceptable standard, a percentage replacement of 10% is suggested for sustainable construction, especially in mass concrete constructions.

## Slide 8
6. Adole, M. A., Dzasu (2011) The empirical investigation reported the effects of chemicals on the properties of concrete with cement partially replaced with Groundnut Husk Ash (GHA). The principal characteristic measured was the compressive strength of Ordinary Portland Cement (OPC) concrete and OPC/GHA concrete after curing in three chemical solutions (MgSO4, NaCl and H2SO4) at 14, 21 and 28 days hydration periods. The results revealed that the OPC/GHA concrete performed best in most of the chemical solutions at 28 days hydration 10 period with compressive strength values of 21.05N/mm2 in MgSO4 solution and 22.55Nmm2 in NaCl solution. The study concluded that OPC/GHA concrete having proven resistant to magnesium sulphate and sodium chloride media would perform better in soils containing MgSO4 and NaCl

## Slide 9: OBJECTIVES
i) To study and determine compressive strength, split tensile strength and flexure strength of concrete.
ii) To identify the proper percentage of alternate materials required for concrete formation in order to improve the hardened properties i.e. strength and durability.
iii) To compare the concrete made with combination of GSA and sisal fiber with the conventional concrete.

## Slide 10
The study comprises of adding ground nutshell ash in cement to improve the compressive as well as tensile strength and sisal fiber for flexure strength of concrete. The whole experiment is carried out in two phases.
In first phase M-30 concrete has been made using 0% GSA i.e. controlled mix is prepared.
The second phase is totally concerned with the partial replacement of cement in M-30 concrete using Groundnut Shell Ash(GSA) at varying percentage i.e. 0%, 5%, 10%, 15% and 20%.Afterwards Adding Sisal fibres at various percentage 0.5%, 1% ,1.5% and 2% in the GSA influenced concrete.
The result obtained from second phase of experiment has been compared with the result obtained from the first phase and analysis has been made.
METHODOLOGY

## Slide 11: RESULTS: Selection of optimum percentage for GSA: A. Compressive Strength
GSA % | Compressive Strength (N/mm2) | 
 | M30 | 
 | 7 Days | 28 Days
GSA 0% | 25.24 | 38.22
GSA 5% | 25.83 | 38.57
GSA 10% | 26.03 | 39.02
GSA 15% | 26.36 | 39.26
GSA 20% | 22.95 | 35.15

## Slide 12
Sisal Fiber Percentage | Compaction Factor
0% | 0.91
0.5% | 0.87
1.0% | 0.85
1.5% | 0.83
2.0% | 0.81
Compaction Factor of Concrete with 15% GSA and Sisal Fiber with various Percentage

## Slide 13
COMPRESSIVE STRENGTH
Sisal Fibre % | Compressive Strength (N/mm2) | 
 | 14 Days | 28 Days
0.0 | 27.51 | 29.62
0.5 | 31.08 | 33.52
1.0 | 35.22 | 38.79
1.5 | 36.47 | 41.48
2.0 | 34.15 | 36.63

## Slide 14
Chart: Compressive Strength (N/mm2)
| 0 | 0.5 | 1 | 1.5 | 2
14 Days | 27.51 | 31.08 | 35.22 | 36.47 | 34.15
28 Days | 29.62 | 33.52 | 38.79 | 41.48 | 36.63

## Slide 15
SPILT TENSILE STRENGTH
Sisal Fiber % | Splitting Tensile Strength (N/mm2) | 
 | 14 Days | 28 Days
0.0 | 2.93 | 3.35
0.5 | 3.51 | 4.09
1.0 | 3.59 | 3.92
1.5 | 3.31 | 3.59
2.0 | 3.08 | 3.38

## Slide 16
Chart: Splitting Tensile Strength(N/mm2)
| 0 | 0.5 | 1 | 1.5 | 2
14 Days | 2.93 | 3.51 | 3.59 | 3.31 | 3.08
28 Days | 3.35 | 4.09 | 3.92 | 3.59 | 3.38

## Slide 17
FLEXURE STRENGTH
Sisal Fiber % | Flexural Strength (N/mm2) | 
 | 28 Days | Percentage Increased
0.0 | 2.7 | -
0.5 | 2.92 | 10
1.0 | 3.41 | 25.13
1.5 | 3.29 | 20.74
2.0 | 3.15 | 15.56

## Slide 18
Chart: Flexural Strength (N/mm2)
| 0 | 0.5 | 1 | 1.5 | 2
28 Days | 2.7 | 2.92 | 3.41 | 3.29 | 3.15

## Slide 19
1.Compressive strength increases as increase in the percentage (%) of Sisal fiber (0% to 1.5%) after 1.5% of SF compressive strength decreases for both 14 days & 28 days cube strength. It was also observed that optimum percentage increment in compressive strength of concrete was 32.3% for 14 days curing and 39.6% after 28 days curing (from 0% to 1.5% addition of Sisal fiber).
2.The optimum percentage increment in split tensile strength was 22.19% for 14 days curing at 1.0% SF and 23.69% for 28 days at 0.5% SF.
3.It was also noted that flexural strength of concrete increase gradually with addition of Sisal fiber and minimum flexural strength was obtained at 0% (2.7 N/mm2). 3.41 N/mm2 optimum flexural strength was obtained with addition of 1.0% Sisal fiber after 28 days of curing
Conclusions:

## Slide 20
DISCUSSION:
Result reveals that the Sisal fibres (SF) reduce early age shrinkage and moisture loss of the concrete mix even when low volume fractions of SF are used. From the result of this research, it was found that the use of fiber in the concrete decreases the workability of the fresh concrete. It was concluded that the increasing percentage volume of fiber added into the concrete would lead the workability decreased. High volume dosage rate above 1.5% showed that the concrete was significantly stiff and difficult to compact and strength also decreases. However, it also reduced the bleeding and segregation in the concrete mixture. Compressive strength of concrete increases with increase in fiber dosage up to 1.5%, then it starts decreasing. The addition of Sisal fibres at low values actually increases the 28 days compressive strength but when the volumes get higher than the 1.5 % SF decreases from original. The tensile strength increases about 23.73 % up to 1.0% after which it decreases. There is about 25.28% increase in flexure strength by adding 1.0% fibres in concrete after which strength starts reducing with further increment in fiber ratios.

## Slide 21
References
IS:2386-1963 (Part-III). Methods of Test for aggregates for concrete Part III specificgravity, density, voids, absorption and bulking. Bureau of Indian Standards.
IS:383-1970. Specification for coarse aggregate and fine aggregate from natural sourcesfor concrete. Bureau of Indian Standards.IS:455-1989. Portland Slag Cement- Specification.Bureau of Indian Standards.
IS:456-2000. Plain and Reinforced concrete- code of practice (Fourth Revision). Bureau of Indian Standards.
IS:456-2000. Plain and Reinforced concrete- code of practice (Fourth Revision). Bureau of Indian Standards.
Jamilu Usman , Nasiru Yahaya , Mohammed Mazizah E2 “Influence of groundnut shell ash on the properties of cement pastes” PSCEE 2019.
Nadiminti Venkata Lakshmi, Polinati Satya Sagar “Study on partial replacement of groundnut shell ash with cement” challenge Journal of Concrete Research Letters · September 2017.
Nigeria T.C. Nwofor and S. Sule “stability of groundnut shell ash (GSA)/ordinary portland cement (OPC) concrete” Advances in Applied Science Research, 2012, 3 (4):2283-2287 ISSN: 0976-8610 CODEN (USA): AASRFC 2283